

FOB Price= 4150 RMB

|  |  |  |
| --- | --- | --- |
| **Specification** |  |   |
| Diameter:  |  | 3.15mm |
| Coil Weight:  |  | 800kg (we can do up to 1000kg) |
| Coil Dimensions: |  | Single Coil of continuous strand (No welded Joins) |
| Carbon: |  | 0.06-0.12% |
| Tensile Strength: |  | 400 – 500 MPa (40-50kg/mm) |
| Elongation: |  | 20%-30% after fracture on 150mm |
| Packing: |  | Strapped Coil,Inner wrap with plastic fillm, outside wrapped with cloth sewn |
| Label: |  | Provided by the customer |
| Internal Diameter: |  | 480mm/630mm |
| External Diameter: |  | 550mm/700mm |